GREEN SAFE SYSTEM_EXTENSIVE HANGING GREENERY_SEDUM
Extensive GreenSafe Sedum hanging system got an average thickness of 13 cm/5,1 inchs and a maximum weight at maximum saturation level of 125 kg/sqm - 275,5 lb/sqm, net of flora.

	SPECIFICATION ITEMS
0.	LAYING SURFACE
	The waterproofing system has to be leak-proof tested and roots-proof certified. / Surfaces have to be clear and clean, without any sharp edge or area, with regular gradients ( > 1%).
1.	ELEMENT OF WATER STORAGE, AERATION, DRAINAGE AND FILTERING
	Modular element STORE MOD, thickness 5 cm (1,96 inches), consist of: retread non-toxic polyester felt 800 gr/sqm weight, size 600/800 mm, with mechanic protection, horizontal and vertical draining function; expanded perlite filling, size 0.1-0.2 mm, with ventilation and store&drain water function; geotextile high toughness polypropylene staple nonwoven cover element,130gr/square meter weight, with filtration and division function from the grown substrate. / Technical Features: / -Thickness: 5 cm; / -Size: 60 x 80 cm; / -pH: 6-7; / -Dry weight: 7 Kg/mq; / -Weight at maximum saturation: 35,00 Kg/m2; / -Water storage capacity: 32 l/m2; / -Storage element porosity: 95%; / -Air Volume at pF1: > 30%; / -Water Volume at pF1: >60%; / -Thermal conductivity lambda: 0.050 W/mk dry; 0.222 W/mk saturation at 100 % / All the elements got CE mark where is needed and comply with UNI11235 law. / GEO GAP and FILTRASAFE supply quantity according to levelling areas (perimeter and emerging parts).
2.	EXTENSIVE GREENING SUBSTRATE
	Extensive greening substrate consist of peat, lapillum, pumice and zeolite laid by an 8 cm/3,1 inch (compaction index included) overall thickness or according agronomic needs of species planted. / Technical features: / Compaction index : 16% / -Size: 0-10 mm; / -Dry apparent volume density: 644 ± 5% kg/m3; / -Weight at potential saturation: 1006 Kg/m3; (*) / -Total porosity v/v: >60%; / -Air volume at pF1: > 15%; / -Water volume at pF1 : > 30%; / -pH: 7-8; / -Electric conductivity: < 50 mS/m; / -Cation exchange capacity > 20 meq/100g s.s; / -Organic Matter: < 60 g/l s.s; / -phytotoxicity eligible; / -Volume reduction grade under compressive strees: ≤16 % / The product comply with UNI 11235:15 law requirements / (*) Maximum saturation at pF 0,7 (UNI EN 13041:2012), Water volume at pF 0,7 > 40 %.
3.	VEGETATION
	Sedum graftable / greening by Crussulacee species like Sedum spp., broadcast sown with a 4 (at least) different species blend e distribuited 80gr/sqm - 3oz/sqm / N.B. Sedum supply could be subjected to seasonal matters , sowing coulb be delayed compered to system laying according weather conditions.
	Sedum Rolls / Sedum rolls greening, made by the cultivation of different species of sedum on a biodegradable pre-vegetated mat, with the aim to get a 90% of surface cover at laying time.
	Sedum pots / greening by Crussulacee species like Sedum spp, 7x7 pots.
4.	IRRIGATION SYSTEM
	Sub-irrigation system consist of a pre-drilled anti-roots 16mm diametr pipe, divided into appropiate areas controlled by 1” 9V bistable solenoid valves and 9V battery control unit, including everything necessary to guarantee the hand-over and acceptance test. (excluding water supply predisposition, which is up to the client).
5.	HANGING SYSTEMS ACCESSORIES
	Inspection drainage concrete sumps, color grey, size 20x20cm, including h 5 cm traps and draining extension in order to achieve hanging package project height.